SECTION 09 2116

GYPSUM BOARD SYSTEMS

*************************************************************************************************************

LANL MASTER SPECIFICATION

This template must be edited for each project.  In doing so, specifier must add job-specific requirements.  Brackets are used in the text to indicate designer choices or locations where text must be supplied by the designer.  Once the choice is made or text supplied, remove the brackets.  The specifications must also be edited to delete specification requirements for processes, items, or designs that are not included in the project -- and specifier’s notes such as these.  To seek a variance from requirements in the specifications that are applicable, contact the Engineering Standards Manual Architectural POC. Please contact POC with suggestions for improvement as well.

When assembling a specification package, include applicable specifications from all Divisions, especially Division 1, General requirements.

Specification developed for ML-4 projects.  For ML-1, 2, and 3 applications, additional requirements and independent reviews should be added if increased confidence in procurement or execution is desired; see ESM Chapter 1 Section Z10 Specifications and Quality sections.

Suspended gypsum board ceiling applications in accordance with this specification, and surrounded by and connected to walls or soffits that are laterally braced to the structure above, need not comply with the seismic sway-bracing requirements of ASCE 7-2010, Chapter 13, paragraph 13.5.6 in accordance with Exception 2.  ASCE 7-2005 paragraph 13.5.6 does not specifically address suspended gypsum board ceiling applications.  ASCE 7-2010 clarifies the requirements between suspended acoustical ceilings and suspended gypsum board ceilings.

*************************************************************************************************************

GENERAL

SECTION INCLUDES

Metal stud wall framing.

Metal channel ceiling framing.

Gypsum board and joint treatment.

Acoustic insulation.

SUBMITTALS

Submit the following:

Catalog data on metal framing, gypsum board, joint tape, joint compound and texturing materials.

Gypsum manufacturer’s documentation of recycled content for gypsum board.

Gypsum manufacturer’s documentation of buyback and/or recycling program.

Submit manufacturer’s written certification that all materials are free of asbestos.

Manufacturer’s installation instructions.

Twelve inch square sample of gypsum board with texture finish.

QUALITY ASSURANCE

Perform work in accordance with ASTM C840, GA-214, GA-216, and GA-600.

REGULATORY REQUIREMENTS

Conform to IBC for fire rated assemblies as follows:

Fire Rated Partitions: Listed assembly UL U465 for 1 hour rating, UL U411 for 2 hour rating.

Fire Rated Ceiling [and Soffits]: Listed assembly UL.

Fire Rated Shaft Walls: Listed assembly UL.]

PRODUCTS

  - product options and substitutions

Comply with Section 01 2500, Substitution Procedures.

  - MANUFACTURERS

Georgia Pacific Corp.

National Gypsum Company.

United States Gypsum Company.

FRAMING MATERIALS

Studs and tracks conforming to ASTM C645 and GA-600; 25 gage galvanized sheet steel, C shape, with knurled faces.

Furring, framing and accessories conforming to ASTM C645 and GA-600.

Fasteners conforming to ASTM C514 and GA-216.

Adhesive conforming to ASTM C557 and GA-216.

GYPSUM BOARD MATERIALS

Recycled Content:  Gypsum recycled content to be the greatest amount available, up to 28 percent post-industrial content.  Subject to compliance with requirements, use synthetic (flue-gas) gypsum when available.  Paper facing to be 100 percent post consumer recycled content.  Fiber gypsum board shall consist of recycled newspaper and gypsum over recycled newspaper, gypsum and perlite core.

Gypsum board conforming to ASTM C1396 and ASTM C1396M, fire resistive, Type X, 5/8 inch thick, maximum practical length, with square cut ends and tapered edges.

Moisture resistant gypsum board conforming to ASTM C630, 5/8 inch thick, maximum practical length, with square cut ends and tapered edges.

Gypsum coreboard conforming to ASTM C442, 1 inch thick, maximum practical length, with square cut ends and tapered edges.

ACCESSORIES

Acoustic insulation conforming to ASTM C665, preformed, formaldehyde-free, glass fiber batts, [2 ¾] [3 5/8] [6 1/2] inches thick, unfaced, friction fit type.

Self-drilling, self-tapping screws, bolts, nuts and washers with hot dip galvanized finish.

Corner beads of metal and paper construction.

Edge bead conforming to ASTM C1047 and GA-216.

Joint materials conforming to ASTM C475 and GA-216; reinforcing tape, joint compound, adhesive (all 100 percent asbestos free) and water.

Latex based texture finish materials.

EXECUTION

  - METAL STUD INSTALLATION

Install studs as indicated on the drawings and in accordance with manufacturer’s instructions and ASTM C754.

Refer to Drawings for locations of studding extending to the ceiling, through the ceiling, and to structure above.

ACOUSTICAL ACCESSORIES INSTALLATION

Refer to Drawings for location of partitions with acoustical treatment.

Install acoustic sealant at joint between gypsum board and floor, and to seal penetrations of partitions by conduit, pipe, ductwork, etc.

Place acoustic insulation between studs, around cut openings, behind and around electrical and mechanical items within or behind partitions, and tight to items passing through partitions.

SHAFT WALL INSTALLATION

Install in accordance with manufacturer’s instructions to GA-600 requirements.

SUSPENDED CEILING GRILLAGE INSTALLATION

Install grillage in accordance with ASTM C754.

Suspend 1-1/2 inch furring channels from structural members with 8 gage wires at 48 inches on center, and within 6 inches of walls.

Install furring channels at right angle to channels [at 16 inches on center] using formed clips.

GYPSUM BOARD INSTALLATION

Install gypsum board in accordance with manufacturer’s instructions.

In non-fire rated partitions, erect single layers of gypsum board in most economical direction, with edges and ends occurring over firm bearing.

In fire rated partitions erect single layer of gypsum board vertically, with edges and ends occurring over firm bearing.

Install screws in accordance with manufacturer’s instructions.

In double layer installations, erect second layer perpendicular to first layer, secured to first layer with adhesive. Offset joints of second layer from joints of first layer.

Treat cut edges and holes in moisture resistant gypsum board with sealant.

Install corner beads at exterior corners.  Install edge trim where gypsum board abuts dissimilar materials.

JOINT TREATMENT

Tape, fill and sand exposed joints, edges and corners to produce smooth surface, ready for finish.

Feather coats onto adjoining surfaces so that camber is maximum 1/32 inch.

TEXTURE FINISH

Apply finish texture coating to attain a light sand finish.

TOLERANCES

Maximum variation of finished gypsum board surface from true flatness is 1/8 inch in 10 feet in any direction.

END OF SECTION

************************************************

Do not delete the following information:

************************************************

FOR LANL USE ONLY

This project specification is based on LANL Master Specification 09 2116 Rev. 2.1, dated April 4, 2012.